## Slide 1: EVALUATION OF FIBER AND YARN TECHNOLOGICAL PROPERTIES OF ADVANCED GREEK COTTON LINES
Dr. Eleni Tsaliki 1, Dr. prof. Mohamed Negm2, Dr. Apostolos Kalyvas1
1 Plant Breeding and Genetic Resources Institute
PO Box 60458 Post code 57001 Thermi Thessaloniki Greece
e-mail: tsaliki@ipgrb.gr
2 Cotton Research Institute, Giza, Egypt

## Slide 2: Cotton - Greek national product
8 % of total agricultural output
More than 55,000 farmers
Average cultivated area 250000 ha (nearly 50% of the irrigated land)
80 % of the EU production

## Slide 3: Cultivation area in Greece 269323,5 ha -2015
Chart: 
| East Macedonia - Thrace | Central Macedonia | Thessaly | Sterea Ellada
Πωλήσεις | 66902.6 | 65566.4 | 94742.4 | 35775.2
Source: www.elstat.gr

## Slide 4: Total Seedcotton yield 817574 tn -2015
Chart: 
| East Macedonia - Thrace (2672 Kg/ha) | Central Macedonia (2744kg/ha) | Thessaly (3402kg/ha) | Sterea Ellada (3217kg/ha)
Total Yield tn | 178767 | 179902 | 322291 | 115091
Source: www.elstat.gr

## Slide 5: www.minagric.gr

## Slide 6: Integrated Management System in Cotton
SEED SELECTION
TILL 60% OPENING OF BOLLS (95 DAYS)
SOWING - FIRST 45 DAYS
DEFOLIATION – HARVESTING - GINNING
AFTER HARVESTING

## Slide 7
201 varieties
Greece 116
Bulgaria 23
Italy 2
Spain 75

## Slide 8: AIM OF THE STUDY
New germplasm is available almost every year and it is important for producers to note genotypic and phenotypic differences in varieties in their region in order to obtain high yields and good fiber quality.
The importance of cotton crop in Greek economy compels plant breeders to make consistent efforts for the genetic improvement of fiber yield and quality.
New varieties with high yield and fiber properties that ensure their commercial success to be included in Greek National Catalogue.

## Slide 9: MATERIALS AND METHODS
2 years, 3 replications, RCB
Seven cotton genotypes developed from cotton breeding programs of the IPBPR and one reference variety
Experimental fields of Plant Breeding and Genetic Resources Institute (IPBPR)
Each plot consisted of two rows of 10 m length and within row spacing were 0.90m

## Slide 10: Cultivation data
 | 2012 | 2013
Sowing date | 22 May | 9 May
Harvesting date | 15 November | 9 October
Min temperature | 3oC (9/11/12) | 8,8oC (27/5/2013)
Max temperature | 39oC (7/8/12) | 37,2 oC (4/8/2013)
Average min temperature | 17,3oC | 18,0oC
Average max temperature | 29,3oC | 30,5oC
Rainfall | 123,3 mm | 94,40mm

## Slide 11
Hand picked and roller ginned

## Slide 12: Cotton fiber evaluation 2012

## Slide 13: Cotton fiber evaluation - 2013

## Slide 14: Lint (%)
Experimental roller gin

## Slide 15: Length (mm) – Maturity index

## Slide 16: Micronaire

## Slide 17: Elongation - Strength

## Slide 18: Colour (Rd-b)

## Slide 19: Lea count strength product (LCSP)
Good-Brand Lea Tester

## Slide 20: Registration of varieties
Application to Variety Research Institute of Cultivated Plants ( V.R.I.C.P.) is a controlling service of the Ministry of Agriculture
8 kg seed (breeder’s category) + fee 1200,00euros
2 years experiments
Registration to National catalogue
Registered variety
certified seeds

## Slide 21
Hellenic Agricultural Organization – DEMETER was established in 2011 following the merge of 4 organizations which are involved in activities in the agricultural sector
HAO –DEMETER functions as a legal entity of the public sector supervised and financed, more than 51%, by the Greek Ministry of Agricultural Development & Food.
After reorganization, in 1/1/2015 the Agricultural Research Centre of Northern Greece, the Institutes of Cotton and Industrial Plants, Plant Protection, Cereals and Pomology have been merged forming the Institute of Plant Breeding and Genetic Resources
    Cereals, 67 varieties of wheat, barley, oat, rice, rye, triticale
    Vegetables, 18 varieties of tomato, egg plant, peppers
    Cotton, 8 varieties
    Tobacco, 34 varieties (unique distributor in Greece)

## Slide 22: THANK YOU FOR YOUR ATTENTION